## Slide 1: USE OF NFC IN PAPERMAKING APPLICATIONS
González, I.; Alcalà, M.; Pèlach, M.A.; Vilaseca, F.; Mutjé, P.
Laboratory of Paper Technology and Polymer Materials (LEPAMAP Group)
Dept. of Chemical Engineering, University of Girona
C/ M. Aurèlia Capmany, 61, 17071 Girona (Spain)
email: fabiola.vilaseca@udg.edu
FPS COST Action FP1105

## Slide 2
Content
INTRODUCTION
PREPARATION OF “OUR” NFC
APPLICATIONS OF NFC IN PAPERMAKING: SOME RESULTS
STRATEGIES APPLIED TO BLEACHED EUCALYPTUS PULPS

## Slide 3
Introduction
Sustainability
Saving of forest resources
Prevent the use of large amounts of virgin fibers
Convert recycling as central part of paper activities
Diminish de basis weight of paper-based products
Major use of fillers (instead of fiber content)
Addition of nanostructures……..NFC!!!!

## Slide 4
Preparation and characterization of NFC
Fiber pretreatment
Refining
Fiber
de-structuring
Homogenizer PANDA 2K-GEA
NFC characterization
Fiber oxidation
Bleached eucalyptus pulp oxidized at neutral pH, TEMPO-mediated.

## Slide 5
Preparation and characterization of NFC
  Degree of polymerization DP = 400
  Carboxylic content CC = 0,4 mmol/g
  Water Retention Value WRV = 17 g/g
  Cationic demand CD = 860 meq-g/g

## Slide 6
Application of NFC – Retention agents
0,5% cationic starch and 0,8% micronized silica
(respect to fiber weight)

## Slide 7
Reixach, R.et al.
BioResources (2013), 8(3):3231-3246
Hubbe, M. A.
BioResources (2014), 9(1):1634-1763
Case Study

## Slide 8
Applications of NFC in papermaking
BLEACHED KRAFT PULP
FROM HARDWOOD
UNBLEACHED KRAFT PULP
FROM HARDWOOD
NFC (%) | ºSR | B.L. (m)
0 | 19 | 3542
3 | 33 | 5508
6 | 55 | 6873
9 | 67 | 7627
NFC (%) | ºSR | B.L. (m)
0 | 18 | 1880
3 | 29 | 3254
6 | 45 | 4365
9 | 54 | 5233
73%
55%

## Slide 9
Applications of NFC in papermaking
RECYCLED DEINKED PULP
MECHANICAL PULP
NFC (%) | ºSR | B.L. (m)
0 | 34 | 1190
1,5 | 40 | 1487
3 | 49 | 1903
4,5 | 55 | 2363
NFC (%) | ºSR | B.L. (m)
0 | 64 | 3326
1,5 | 80 | 4650
3 | 84 | 5068
4,5 | 87 | 6054
50%
60%

## Slide 10
CTMP FROM RAPESEED RESIDUES
Applications of NFC in papermaking
NFC (%) | ºSR | B.L. (m)
0 | 52 | 2609
3 | 62 | 3350
6 | 78 | 3827
9 | 88 | 4473
73%
In all cases, 6-9wt% of NFC would be desirable, regarding the improving on physical properties.
Chart: 3wt% NFC
| Bleached | Unbleached | Recycled | Mechanical | CTMP fr residue
Serie 1 | 3254 | 5508 | 4650 | 1903 | 3350

## Slide 11
STRATEGIES FOR EUCALYPTUS PULP
Bleached
virgin fibers
Mild beating
Bio-beating
NFC
in bulk
NFC
NFC
NFC
at surface
(I)
(II)
(III)
González, I. et al.
BioResources (2012), 7(4):5167-5180
González, I. et al.
Cellulose (2013), 20:1425-1435
Unpublished results
Goal: 33-35 ºSR (drainage)

## Slide 12
0% NFC bulk
LR = 1880 m
ºSR = 16
3% NFC bulk
LR = 3360 m
ºSR = 33
0,45% NFCsurf
in water
LR = 4709 m
0,45% NFCsurf
in starch
LR = 6008 m
NFC
in bulk
NFC
at surface
(III)
Strategies for eucalyptus pulp
TEMPO at basic pH
Highly oxidized
NFC applied at surface:

## Slide 13
Chart: Breaking Length (m)
| 0% NFC bulk | 3% NFC bulk | 0,45% NFC surf (water) | 0,45% NFC surf (startch)
Serie 1 | 1880 | 3360 | 4709 | 6008
1880
3360
4709
6008
NFC
in bulk
NFC
at surface
(III)
Strategies for eucalyptus pulp

## Slide 14
Strategies for eucalyptus pulp
NFC
in bulk
NFC
at surface
(III)
Chart: Surface NFC
| NFC - 0,5 meq-COOH/g | NFC - 1,4 meq-COOH /g | NFC - 1,7 meq-COOH/g
Serie 1 | 4756 | 6008 | 5616
4756
5616

## Slide 15
Strategies for eucalyptus pulp
Relationship between oxidation level and degree of polymerization:
Shinoda, R. et al. BioMacromolecules (2012), 13:842-849

## Slide 16
Conclusions and challenges
Forthcoming challenges:
Mineral particles (fillers) retention??? Role of NFC ???
Use of retention agents and drainage agents to improve drainage

## Slide 17: USE OF NFC IN PAPERMAKING APPLICATIONS
Fabiola Vilaseca
email: fabiola.vilaseca@udg.edu

## Slide 18
Strategies for eucalyptus pulp
Relationship between oxidation level and degree of polymerization:
Shinoda, R. et al. BioMacromolecules (2012), 13:842-849
The degree of polymerization is affected by the carboxylic content