## Slide 1: Quantitative analysis of complex oligomeric mixtures by MS
Sheetal Gangula, Institute of Food chemistry

## Slide 2
WHAT
Distribution of substituents along the polymer chain
  random distribution?
  high and low substituted areas?
WHY
structure-property relationships
  E.g. thermo-reversible gelation
HOW
quantitative mass spectrometry (MS) of oligomers
Quantitative Analysis of Cellulose Ethers
Notes: problems partial hydrolysis

## Slide 3
Quantitative MS of Methyl Cellulose
methyl cellulose
CH3
CD3
permethylation
with CD3I
partial degradation to oligomers
mass spectrometric analysis
R. Adden et al., Macromol. Chem. Phys., 207 (2006) 954-965
number of
[M+Na]+
[M+Na]+
Notes: problems partial hydrolysis

## Slide 4: Analysis by MS
QUALITATIVE ANALYSIS
Peak Identified by m/z value
QUANTITATIVE ANALYSIS
Depends on peak intensity
But this is not simple as peak intensity varies depending on chemistry,instrumental parameters and mass differnce
4

## Slide 5: Analysis by MS
For example different compounds at equimolar concentrations give different peak intensities
So for quantitative evaluation behaviour of different compounds with respect to chemistry and instrumental parameters has to be studied
Mass spectrum from ESI-IT-MS
m/z-
m/z-
DP2-Me
DP2-Et
The samples are seen as sodium adducts M+Na+ in MS
5

## Slide 6: Our current study
preparation of a roughly equimolar
oligosaccharide mixtures
determination of the
exact composition
Evaluation of sodium adducts in mass spectrum
ESI-IT MS
MALDI-ToF-MS
Samples measured under defined conditions
6

## Slide 7: Sample Preparation
2,3,6-O-Me-β-CD
2,3,6-O-Med3-β-CD
2,3,6-O-Et-β-CD
Reductive amination
Mixture of oligosaccharides
(DP1-DP7) are obtainted from each sample
Mixture of oligosaccharides
(DP1-DP7) after
reductive amination
LC/UV
Partial hydrolysis
7

## Slide 8: Types of mixtures
Three types of mixtures are presented :
Methylated and deuteromethylated oligomeric mixtures (Me,Med3)
Methylated and ethylated oligomeric mixtures (Me,Et)
Deuteromethylated and ethylated oligomeric mixtures (Med3,Et)
8

## Slide 9: ESI-IT-MS (electrospary ionization mass spectrometry)
9

## Slide 10: Results from ESI-IT-MS
Results are expressed as relative ion intensities. This is obtained by dividing the intensity of one compound in mass spectra by another compound w.r.t a certain DP in a mixture.
Me,Med3 mixture Me,Et mixture Med3,Et mixture
Chart: Relative ion intensity Med3/Me
| RI
 | 1.09

 | 0.92125

 | 0.96
Chart: Relative ion intensity Et/Me
| RI
 | 3.37

 | 2.68

 | 2.69
Chart: Relative ion intensity Et/Med3
RI | 3.25 | 2.53 | 2.48
10

## Slide 11: COST action FP1105 STSM
MALDI-ToF-MS:
Measurements were performed at:
The institute of Polymer Technology at KTH Royal Institute of Technology, Stockholm
Instrument used:
Bruker Daltonics Ultraflex

## Slide 12: MALDI-ToF-MS (matrix assisted laser desorption mass spectrometry)
11
sDHB

## Slide 13: Selection of laser power
Me,Et
Me,Med3
LP 40 %
LP 45 %
LP 50 %
LP 50 %
LP 55 %
LP 60 %
12

## Slide 14: Results from MALDI-ToF-MS
Chart: Average relative ion intensity
| RI
 | 1.03

 | 0.99

 | 0.99
DP2
Chart: Average relative ion intensity
| RI
 | 1.585

 | 1.9633

 | 1.6383
Chart: Average relative ion intensity
| RI
 | 1.86

 | 2.29

 | 1.91
DP2
Results are expressed as relative ion intensities. This is obtained by dividing the intensity of one compound in mass spectra by another compound w.r.t a certain DP in a mixture.
Me,Med3 mixture Me,Et mixture Med3,Et mixture
13

## Slide 15: SUMMARY
Under optimal conditions for both instruments...
Me and Med3 oligosaccharides are similar in polarities, hence their relative ion intensities
in mass spectra are almost 1:1 with a little scattering for various DP. The scattering of data is lees in MALDI-ToF-MS compared to ESI-IT-MS.
Polarity of Et oligosaccharides is lower than that of Me-derivatives and Med3-derivatives,
these compounds in
ESI-IT-MS:
    show 3-4 times higher intensities, but this factor is decreasing with DP
MALDI-ToF-MS:
    the factor is scattering around 1.5-2.5, but it has no clear trend. May be since there is difference in polarities of the compounds they may have different interaction with matrix so the scattering is higher. This has to be further investigated.
14

## Slide 16
Thank you for your kind attention
15