## Slide 1
Thermal properties of different hardwood species
COST FP1105 Meeting, San Sebastian, 26-27.05.2015
Carmen-Mihaela Popescu, Maria-Cristina Popescu
”Petru Poni” Institute of Macromolecular Chemistry of Romanian Academy, Iasi, Romania

## Slide 2
Purpose
Provide information concerning components composition and thermal properties of different hardwood species

## Slide 3
Materials
Species | Average wood density | Average component percentage (%) |  | 
 |  | Cellulose | Lignin | Hemicelluloses and others
poplar (Populus tremula) | 0.45 | 48-49 | 21-25 | 26-31
lime (Tillia cordata) | 0.48 | 48-51 | 20-22 | 27-32
cherry (Prunus avium) | 0.50 | 45-47 | 18-21 | 32-37
maple (Acer pseudoplatanus) | 0.56 | 45-47 | 19-22 | 31-36
http://www.worldagroforestrycentre.org/sea/Products/AFDbases/WD/, R. B. Hoadley. Physical and chemical properties, in: Identifying wood. Accurate results with simple tools, Taunton Press, U.S., 1990, pp. 46-53, R. M. Rowell, R. Pettersen, J. S. Han, J. S. Rowell, M. A. Tshabalala, Cell Wall Chemistry, in: Handbook of wood chemistry and wood composites, ed. R. M. Rowell, CRC Press, 2005

## Slide 4
Methods
Thermogravimetry
Infrared spectroscopy
Two dimensional correlation infrared spectroscopy

## Slide 5
Thermal methods
evaluation of the thermal stability and degradation degree as a function of the content of the obtained fractions
investigation of wood structural components
estimation of the kinetic parameters
thermal “fingerprints”
molecular arrangements and interaction between wood components
TG + IR + 2DCOS

## Slide 6
Termogravimetry
Species | Step II |  |  |  | 
 | Ti | Tsh | Tm | Tf | W%
poplar (Populus tremula) | 153.7 | 287.2 | 359.0 | 525.8 | 74.8
lime (Tilia cordata) | 150.0 | 289.9 | 356.2 | 525.3 | 71.6
cherry (Prunus avium) | 153.9 | 290.5 | 353.3 | 519.6 | 71.0
maple (Acer pseudoplatanus) | 147.6 | 301.5 | 351.5 | 524.3 | 72.2
hemicelluloses
cellulose
lignin

## Slide 7
Termogravimetry

## Slide 8
Infrared spectroscopy

## Slide 9
Infrared spectroscopy

## Slide 10
Infrared spectroscopy

## Slide 11
Infrared spectroscopy
20 → 220 oC (with 1 oC/min)

## Slide 12
Infrared spectroscopy
PT
TC
PA
AP
20 oC
220 oC

## Slide 13
Infrared spectroscopy
PT
TC
PA
AP

## Slide 14
Infrared spectroscopy
PT
C–O in quinines and C=O in various groups → degradation of the acetyl groups and formation of other structures
C=C in aromatic skeletal components in lignin → increase of the amount of lignin due to degradation of amorphous carbohydrates
C–O of Ph–O–C in lignin and C–O in xyloglucan → loss of acetyl groups

## Slide 15
sample
spectrum
electro-magnetic beam
External perturbation (temperature)
dynamic
Two dimensional (2D) correlation spectroscopy

## Slide 16
Synchronous 2D correlation spectra represent the simultaneous or coincidental changes of spectral intensities measured at the wavenumbers 1 and 2
The diagonal peaks are referred to as – “autopeaks” 1=  2
The peaks located at the off–diagonal positions are referred as – “crosspeaks” 1  2
n1
n2
crosspeaks
autopeak
-
+
2D IR correlation spectroscopy

## Slide 17
Sequential, changes of spectral intensities at the wavenumbers 1 and 2. The spectrum is antisymmetric with respect to the diagonal line.
The peaks located at the off–diagonal positions are referred as – “crosspeaks” 1 2
n1
n2
crosspeaks
-
+
2D IR correlation spectroscopy

## Slide 18
Simplification of complex spectra and enhancement of spectral resolution
Detailed investigation of the intra- and intermolecular interaction
Study of the process of chemical reaction or the kinetics of molecular vibrations
Band assignments based on the correlation analysis between various bands
Advantages

## Slide 19
2D IR correlation spectroscopy

## Slide 20
2D IR correlation spectroscopy
PT
TC
PA
AP
3287 > 3343 > 3456 cm-1

## Slide 21
2D IR correlation spectroscopy

## Slide 22
2D IR correlation spectroscopy
PT
TC
PA
AP
1720 > 1739 , 1558 > 1605 > 1651, 1504,
1538 > 1636 > 1785 cm-1

## Slide 23
Conclusions
Thermogravimetry indicated the thermal properties of the studied wood samples.
The calculated percentages of the components are in good correlation with the values from literature data.
The ratio values of lignin/carbohydrate IR bands decrease and of carbonyl/carbohydrate IR bands increases with increasing the average wood density.
The infrared and 2DCOS IR spectra indicates structural modifications (induced by different reactions) in the main components of wood.

## Slide 24
Thank you for your attention!

## Slide 25
Questions?
Iasi