## Slide 1: Hybrid Nanocellulose-Clay Composites for Controlled Release
Supervisors: Peter SZABO, Anders Egede DAUGAARD, Ole HASSAGER
ESR: Jon TRIFOL GUZMAN
Danish Polymer Center
Department of Chemical and Biochemical Engineering
Technical University of Denmark
Kongens Lyngby, Denmark

## Slide 2: INTRODUCTION
  - PLA (Polylactic acid)
    Renewable source
    Biodegradable
    Suitable for industry
    Good Mechanical properties
    Transparent
    ~ Cost
    Barrier properties
    Thermomech. properties
    Slow crystallization
    Brittleness
NANOCOMPOSITE
C30B
CNF
Improvement of properties?
Comparisson vs
Synergetic
When? How? How much?
NEED TO
BE FIXED

## Slide 3: NANOCELLULOSE PRODUCTION
STABLE SUSPENSION

## Slide 4: NANOCELLULOSE PRODUCTION

## Slide 5
PLA BASED NANOCOMPOSITES
PLA & PLA +
C30B
PLA +
CNF
PLA +
CNF +
C30B
DMF + 15 h 80 °C
DCM
15 h 23 °C
SOLVENT CASTING  BETTER FOR THE ”PROOF OF THE HYPOTHESIS”
 ”UPSCALING”  NEXT RESEARCH  MULTIPLE POSSIBILITES
BEST CONDITIONS FOR EACH NANOCOMPOSITE

## Slide 6: TRANSPARENCY
HOT PRESSED
NANOCOMPOSITES
PLA/CNF 1%/C30B 1% TRANSPARENT
AND CLEAR
INFRARED
UV
UV
BLOCKING?

## Slide 7: CRYSTALLIZATION: XRD, MDSC & POM
PLA/C30B 1%
t1/2 = 3 min
PLA CNF 1%
t1/2 = 9 min
PLA CNF 1%
C30B 1%
t1/2 = 5 min
PLA
t1/2 = 25 min
Kinetic  IMPROVEMENT
Size and shape  ?

## Slide 8: THERMOMECHANICAL PROPERTIES
Neat PLA
PLA CNF/C30B
1% 1%
There is also a synergetic behaviour
The improvement is really meaningful even at low load
PLA CNF 5%

## Slide 9: BARRIER PROPERTIES
PLA/CNF 5%/C30B 5%
89% REDUCTION OTR
75% REDUCTION WVTR

## Slide 10: POLARIZED OPTICAL MICROSCOPY
PLA | PLA C30B 1% | PLA CNF 1% | PLA CNF C30B 1%
AFTER SOLVENT CASTING |  |  | 
AFTER ISOTHERMAL CRYSTALLIZATION @ 100 C (COMPARABLE DEGREE OF CRYSTALLINITY) |  |  | 
100 µm
100 µm
100 µm
100 µm
100 µm
100 µm
100 µm
100 µm

## Slide 11: CRYSTALLINITY AND BARRIER PROPERTIES
PLA
PLA/C30B 1%
PLA/CNF 1%
PLA/CNF/C30B 1% 1%
SOLVENT CASTING
AMORPHOUS
FULLY CRYSTALLIZED
5 MINUTES AT 170 °C - FAST COOLING
120 MINUTES 120 °C
AMORPHOUS MOBILE/RIGID 
UNDER INVESTIGATION

## Slide 12: WATER DIFFUSIVITY
DIFFUSIVITY
CONTROLLED
QUARTZ SPRING MICROBALANCE

## Slide 13: GRAFTING OF BZAA (SOLREACT)
+
Small vacuum
T= 130 °C
Tb(water) < T < Tb (agent to graft)
Removal of water  critical!
Not removal of the agent to graft
Acetate groups  acetic acid  removed ?
ABSORBANT
Improve dispersion
+
GIVE AN EXTRA FUNCTION
ESTERIFICATION

## Slide 14: CONTROLLED RELEASE
95% MeOH on water  fatty food simulant.
PLA + 6% CARVACROL
PLA CNF 3% + 6% CARVACROL
PLA gCNF 3% + 6% CARVACROL
PLA gCNF 3% C30B 5% + 6% CARVACROL
SOLVENT CASTING
ISOTHERMAL
CRYSTALLIZATION
7,5 min at 120 ºC

## Slide 15: CONTROLLED RELEASE
BAD CLAY
DISPERSION!

## Slide 16: INTRODUCTION
  - PLA (Polylactic acid)
    Renewable source
    Biodegradable
    Suitable for industry
    Good Mechanical properties
    Transparent
    ~ Cost
    Barrier properties
    Thermomech. properties
    Slow crystallization
    Brittleness
NANOCOMPOSITE
C30B
CNF
Improvement
of properties?
Comparisson vs
Sinergetic
When? How? How much?
NEED TO
BE FIXED

## Slide 17: INTRODUCTION
  - PLA (Polylactic acid)
    Renewable source
    Biodegradable
    Suitable for industry
    Good Mechanical properties
    Transparent
    ~ Cost
    Barrier properties
    Thermomech. properties
    Slow crystallization
    Brittleness
NANOCOMPOSITE
C30B
CNF
Improvement
of properties?
Comparisson vs
Sinergetic
When? How? How much?
ENHANCED
ENHANCED
ENHANCED
MANTAINED
ENHANCED

## Slide 18
Langowski, H.-C., (2008) Permeation of Gases and Condensable Substances through Monolayer and Multilayer Structures. In: Plastic Packaging: Interactions with Food and Pharmaceuticals (Eds. Piringer O.G., Baner A.L.) 2008: Wiley-VCH, 297-347.

## Slide 19: ACKNOWLEDGEMENTS
To my supervisor board for guiding me during my PhD.
To my coauthors for helping me and their valuable advices.
In memoriam to Prof. Iñaki Mondragón Egaña, whose dedication for the science is a inspiration for me.
To the Marie Curie (ITN) Program (Project: NewGenPak project No: 290098) for the financial support.
To this COST Action FP1105 for the invitation to several meetings where I have learnt a lot (I got some inspirations during meeting at Thesalonniki)