## Slide 1: Control of protein affinity in bioactive nanocellulose by passivation with PDMAEMA-block-POEGMA copolymers and false positive response
Maija Vuoriluoto1, Hannes Orelma1, Leena-Sisko Johansson1, Baolei Zhu2, Mikko Poutanen3, Andreas Walther2, Janne Laine1, Orlando J. Rojas1
1Bio-based Colloids and Materials (BiCMat), Department of Forest Products Technology, Aalto University, School of Chemical Technology, Espoo, Finland
2DWI − Leibniz-Institute for Interactive Materials Research, Aachen, Germany
3Department of Applied Physics, School of Science, Aalto University, Espoo, Finland

## Slide 2: Motivation
Non-specific protein adsorption limits the accuracy and selectivity of biosensors
Multifunctional polymers containing poly(ethylene glycol) (PEG) molecules effective in preventing non-specific surface protein adsorption
Cellulosic materials are appealing substrates for biomedical applications
http://technologyinscience.blogspot.fi/2012/12/rapid-diagnostic-tests-types-strength.html
http://www.early-pregnancy-tests.com/inpregtesstr.html
http://uk.clearblue.com/clearblue-pregnancy-tests-range/clearblue-plus-pregnancy-test
Notes: Cellulose is hydrophilic, biodegradable, biocompatible, available etc.
  ELISA based biassays, microfluidic devices, rapid tests
Target analyte should react specifically with the capture agent not the whole substrate
Here we present a method to create low fouling TEMPO-CNF surface with block copolymer

## Slide 3: Structure of PDMAEMA-block-POEGMA copolymers analyzed
Chart: Monomers
| D33-EGMA52 | D33-EGMA137 | D58-EGMA10 | D58-EGMA118 | D74-EGMA17 | D74-EGMA118
PDMAEMA | 33 | 33 | 58 | 58 | 74 | 74
POEGMA | 52 | 137 | 10 | 118 | 17 | 118
RAFT polymerization of:
PDMAEMA = poly(2-(dimethylamino)ethyl methacrylate)
  Quaternized by methyl iodide
POEGMA = poly(oligo(ethylene glycol)methyl ether methacrylate)
  Highly hydrophilic due to PEG units
D33-EGMA52
D33-EGMA137
D58-EGMA118
D58-EGMA10
D74-EGMA17
D74-EGMA118
PDMAEMA
POEGMA

## Slide 4: Reduction in human IgG adsorption on TEMPO-CNF with blocking agents
Chart: Adsorbed hIgG (mg/m²)
| 0.55206707374138964 | 0.3650713606247708 | 0.19156904831276153
lyhyt | 12.4559 | 10.6396 | 9.5647 | 3.1186 | 0.5451 | 1.4955 | 1.9309
pitkä | -0.23266 | 0.47838 | 0.54092
TEMPO-CNF
(REF)
D33-EGMA52
D33-EGMA137
D58-EGMA10
D58-EGMA118
D74-EGMA17
D74-EGMA118
SuperBlock
BSA
PEG-amine
Blocking efficiency %
96 %
100 %
96 %
88 %
85 %
96 %
15 %
23 %
75 %
Adsorbed amount
after blocking with

## Slide 5: Thank you!